## Slide 1
Development and testing of a physically-informed artificial neural network potential for the silicon system
James Hickman*, Ganga Purja Pun**, Francesca Tavazza*, Yuri Mishin**
*National Institute of Standards and Technology: Materials Measurement Laboratory (MML). ** George Mason University: Department of Physics
contact: james.hickman@nist.gov
structure
The present work focuses on the development of a new type of classical interatomic potential known as a “physically-informed neural network” (PINN) potential. This novel format combines the high level of accuracy and flexibility associated with artificial neural networks (ANNs) with the transferability inherent to physical analytic potential models. We focus on silicon as a test case, however, the PINN model can generally be applied to any multicomponent metallic or covalently bonded material.
Introduction
Motivation
All computational methods have associated limitations and compromises. Therefore, models which mitigate these compromises open up new avenues of exploration and enable the discovery of novel phenomena.
Computational material science spans a wide range of length and time scales ranging from the sub-atomic to the macroscopic. In the present work we focus on the atomistic domain, particularly, density functional theory (DFT) and classical methods such as molecular dynamics (MD) or Monte Carlo (MC).
Ab-initio/DFT
Classical (MD/MC)
Slow
Size limited (N~ )
0K or short timescales
Very accurate
Speed
Accuracy
Scalability
Transferability
Compromises
Classical
MD/MC
Computationally Fast [5]
Larger systems (N~ )
Kinetic phenomena/long simulations
Accuracy depends on approximation of the potential energy surface (PES)
Reference [1]
Types of interatomic potentials
Slow relative to traditional potentials
Same benefits as straight NN
Decent extrapolation
Potential models derived from physics
Pro’s
Con’s
Many methods for approximating the potential energy surface exist; collectively these methods are known as interatomic potentials. Typically such methods predict the energy of each atom and sum these individual contributions to get the total structural energy. Below are three commonly used schemes.
Traditional Potentials: (physical model)+(parameterization)
computationally fast
Decent extrapolation
Potential models derived from physics
Difficult to train/fit
Hard to improve upon once finalized
Accuracy limitations
Atom-i
Neighbor list
parameterization
interatomic
potential
model
atomic energy
Pro’s
Con’s
Reference [2]
Mathematical neural network potentials: [3]
NN
local structure
parameters for atom-i
Pro’s
Fast relative to DFT
DFT level accuracy (~1-5 mEv) within training set
Relatively straight forward and routine to train/fit
Systematic improvement (add more data)
Con’s
Slow relative to traditional potentials
Bad extrapolation
Atom-i
Physically informed neural network (PINN) potentials: [4]
NN
Neighbor list
interatomic
potential
atomic energy
Atom-i
local structure
parameters for atom-i
parameterization
Physically informed neural network potentials
References
[1] Image source: http://evolution.skf.com/us/bearing-research-going-to-the-atomic-scale
[2] Image source: https://glossary.periodni.com/glossary.php?en=Lennard-Jones+potential
[3]. Behler, Jörg, and Michele Parrinello. "Generalized neural-network representation of high-dimensional potential-energy surfaces." Physical review letters 98.14 (2007): 146401
[4] Pun, G. P., Batra, R., Ramprasad, R., & Mishin, Y. (2018). Physically-informed artificial neural networks for atomistic modeling of materials. arXiv preprint arXiv:1808.01696.
[5] Plimpton, Steve. "Fast parallel algorithms for short-range molecular dynamics." Journal of computational physics 117.1 (1995): 1-19.
[6] Kresse, G., and J. Furthmüller. "Software VASP, (1999).” Phys. Rev. B 54.11 (1996): 169.
[7] Pun, GP Purja Physical Review B 95.22 (2017): 224103.
Neural Network training
DFT training set generation:
Structures
DFT energies
Model energies
structure-1
structure-2
structure-N
“Training set”
Model error
Fit the NN weights and bias’s
to minimize the RMSE
Training process:
In the present work we utilize the PINN interatomic potential formalism [4]. This model can be broken into three separate parts as summarized below.
Functional/PP: PBE/PAW
ENCUT=600 eV
~4300 structures
block size 1-96 atoms
k-point convergence
VASP:
2D Silicene allotropes
Bulk phase
Atomic clusters
Surfaces
Interstitials, vacancies, stacking faults
Conclusions
  We developed a new silicon interatomic potential using the PINN potential format
  Even in preliminary stage we are obtaining excellent agreement with the DFT energies
  Current potential reproduces DFT data around 300x better than current traditional potentials
Local Structural “Finger-printing”
(neural network input)
i
j
k
form neighbor
list
Angular term
Radial term
Results
Results
Property comparison:
Comparison with Traditional potentials
Comparison with NN potentials
Phonon density of states
Note: From Previous PINN version
Liquid RDF
Thermal expansion
(https://jarvis.nist.gov/)
[7]
[7]
[7]
2591
Modified Tersoff
PINN
Stillinger-Weber
RMSE (meV/atom)
1281
5
[7]
Select equations of state
Tetrameter
Silicene
Bulk phases:
diamond
FCC
SC
BC8
Deviation from DFT(%)
physical extrapolation
catastrophic
extrapolation!!
physical extrapolation
catastrophic
extrapolation!!
Training region
zoom
Distribution of training error
Training data
RMSE= 4.95 meV
Distribution of validation error
Validation data (untrained)
RMSE= 5.58 meV
y=x equality with DFT
input layer
hidden layers
output
layer
final layer has no
transfer function
Neural network evaluation
Physical model evaluation
The weights and bias are the NN’s fitting parameters
NN Architecture: 60x32x8
Artificial neuron
(nodes or perceptrons)
weighted and
biased signal
transfer
function
input signals
neuron
output
8 Adjustable terms which are controlled by the outputs of the NN
Cutoff function
repulsive term
promotional energy
screening factor
number of chemical bonds
bond order parameter
liquid
bulk
SL
interface
GB
vacancy
(Legendre polynomials)
Quantum
DFT
Coarse Grained
Continuum
FEM
attractive term
Notes: Behavioral results: make bar graphs of RT?
fMRI results: labels, figure caption, make blues in graph the same color
References: add marcel 2004, add numbers, rearrange